GUIDE SPECIFICATION FOR CEM-KOTE® FLEX ST:  FLEXIBLE CEMENTITIOUS WATERPROOF COATING

07 16 00 – Cementitious and Reactive Waterproofing

Specifier Notes: This guide specification is written according to the Construction Specifications Canada (CSC) format. The section must be carefully reviewed and edited by the Architect or Engineer to meet the requirements of the project. Coordinate this section with other specification sections and drawings.

Specifier Notes: This specification is for the installation of CEM-KOTE FLEX ST, flexible, cementitious waterproofing coating in new construction. CEM-KOTE FLEX ST is designed for positive and negative waterproofing of concrete structures in new construction and restoration. It is suitable for water and wastewater tanks, secondary containment structures, tunnels, concrete slabs, balconies, and patios with light-to-medium traffic. In new construction, where superior flexibility is required (i.e., waste water treatment facilities), CEM-KOTE FLEX ST can be reinforced with REINFORCING FABRIC HD throughout. In restoration, REINFORCING FABRIC NW is used just over the cracks to provide bridging. This specification should be read in conjunction with both the product data sheets and installation instructions. CEM-KOTE FLEX ST is approved for use in potable water facilities as per ANSI/NSF Standard 61 – Barrier Materials.

1		GENERAL

1.1		SECTION INCLUDES

.1	Surface preparation.

.2	Application of a flexible, cementitious, waterproofing coating.

.3	The general conditions, supplementary conditions, and general requirements of this document apply to general contractors, subcontractors, material suppliers, and all other persons furnishing labour and materials under this section.

1.2		WORK INCLUDED

.1	Provide all labour, material, and equipment necessary to apply cementitious coating in application over concrete surfaces as shown on the contract drawings and specified herein.

Specifier Notes: The concrete surfaces in new construction may have “bug holes,” poor compaction areas, “honeycombing,” “form displacements,” and other imperfections. These may have to be repaired/leveled prior to application of CEM-KOTE FLEX ST waterproofing system.  The project specification must identify the responsibility for leveling these imperfections.

1.3		RELATED SECTIONS

Specifier Notes: Edit the list of related sections as required for the project. List other sections dealing with work directly related to this section.

.1	Section 03 30 00 – Cast-In-Place Concrete.

.2	Section 03 01 30.61 – Rehabilitation of Cast-in-place Concrete.

.3	Section 07 10 00 – Dampproofing and Waterproofing.

1.4		REFERENCES

.1	ASTM C672 - Standard Test Method for Scaling Resistance of Concrete Surfaces Exposed 		to De-Icing Chemicals.

## .2	ASTM D412 (modified) - Standard Test Methods for Vulcanized Rubber and Thermoplastic 		Elastomers—Tension.

.3  	ASTM E96 - Standard Test Methods for Water Vapor Transmission of Materials ("Wet Cup" 		Procedure).

.4	TT-P-1411 – Federal Specification, Paint, Copolymer-Resin, Cementitious (for Waterproofing 			Concrete and Masonry Walls).

.5	Gemite ISO TP (Test Procedure) 005-97 - Tensile Properties of Thin Cement Composites.

1.5		QUALITY ASSURANCE

.1	Contractor will provide the proper equipment, manpower, and supervision at the jobsite to install the cementitious coating in compliance with the project plans and specifications.

.2	Prepare a site sample approximately 1200 mm x 1200 mm.  This sample will be regarded as the minimum standard of workmanship acceptable for this project.

### .3	The installation should be carried out by an approved applicator of Gemite Products Inc.  			Key tradesmen on the site must be well qualified in the product mixing and application 			procedures.

.4	Installation must be carried out by an experienced contractor with an adequate number of 		skilled personnel, experienced in the application of the cementitious coating systems.

.5	Maintain a record of the batch numbers of all materials supplied for this project.

1.6		PRE-CONSTRUCTION MEETING

.1	Convene [one] [_____] week [____] prior to commencing work of this section, in accordance 		with Section 1.05 - Quality Assurance, meeting with manufacturer’s technical representative, 		General Contractor and Site Engineer to review the installation procedures.

1.7		SUBMITTALS

.1	Comply with Section 01 33 00 - Submittal Procedures.

.2	Submit manufacturer's product data and application instructions.

1.8		DELIVERY, STORAGE, AND HANDLING

.1	Deliver materials to site in manufacturer's original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

### .2	Store cementitious coating in a clean, dry area protected from direct sunlight, weather and 		other damage.  Store all wet materials at a temperature of not less than 5o C at all 			times.

### .3	Protect materials during handling and application to prevent damage or contamination.

1.9		ENVIRONMENTAL REQUIREMENTS

.1	Product not intended for uses subject to abuse.

.2	Product must never be applied if ambient temperatures cannot be kept above 4o C during application and for 48 hours thereafter.

.3	Avoid applications at temperatures above 28o C.

.4	Protect surrounding surfaces from damage due to work of this trade.

### .5	Hot Weather Application

### .1	Protect the surface against rapid evaporation of water between the finishing and the 			final set time.

### .2	Use water misting or apply a surface evaporation retarder.

### .6	Cold Weather Application

### .1	Apply in temperatures above freezing point.

### .2	Protect the material against freezing for a minimum of 48 hours.

### .3	Use electrical heaters to avoid carbonation and carbonation cracking.

2		PRODUCTS

2.1		MANUFACTURER

.1	W. R. MEADOWS OF CANADA, 70 Hannant Court, Milton, Ontario, Canada  L9T 5C1.

(800) 563-3618. Fax (905) 878-4125. Website:  www.wrmeadows.com.

.2	GEMITE PRODUCTS INC., 1787 Drew Road, Mississauga, Ontario, Canada L5S 1J5.  (888) 443-6483.  Fax (905) 672-6780.  Website:  www.gemite.com.

2.2		MATERIALS

.1	Flexible Cementitious Coating:  CEM-KOTE FLEX ST manufactured by Gemite Products Inc., and distributed by W. R. MEADOWS.

2.3		ACCESSORIES

.1	Reinforcing Fabric (Woven) for cove reinforcement or entire surface application:  REINFORCING FABRIC HD manufactured by Gemite Products Inc., and distributed by W. R. MEADOWS.

.2	Reinforcing Fabric (Non-Woven) for crack treatment: REINFORCING FABRIC NW manufactured by Gemite Products Inc., and distributed by W. R. MEADOWS.

.3	Bonding Mortar for coves on protruding steel and plastic pipes:  CEM-KOTE BARRIER COAT 100 manufactured by Gemite Products Inc., and distributed by W. R. MEADOWS.

.4	Thin Patching Mortar for thin repairs, including bug holes:  MEADOW-PATCH™ T1 manufactured by W. R. MEADOWS.  For spray application, use CEM-KOTE FLEX ST manufactured by Gemite Products, and distributed by W. R. MEADOWS.

.5	Overhead/Vertical Structural Repair Mortar for repairs or coves:  MEADOW-CRETE® OV manufactured by W. R. MEADOWS.

.6	Thin-Set Concrete Finishing Mortar:  GEM-PLAST TC manufactured by Gemite Products Inc., and distributed by W. R. MEADOWS.

.7	Horizontal Structural Repair Mortar:  MEADOW-CRETE H manufactured by W. R. MEADOWS.

3		EXECUTION

3.1		EXAMINATION

.1	Examine surfaces to receive the flexible cementitious coating.

### .2	Report to owner's representative, in writing, any defects in previously prepared Work, or 			unsatisfactory site conditions.

Specifier Notes:  The concrete surfaces in new construction may have “bug holes,” poor compaction areas, “honeycombing,” form displacements, and other imperfections.  These may have to be repaired/leveled prior to application of the CEM-KOTE FLEX ST waterproofing system.  The project specification must identify the responsibility for leveling these imperfections.

.3	Do not begin surface preparation or application until unacceptable conditions have been corrected.

.4	Starting work under this section means acceptance of the surface and previously prepared work.

3.2		SURFACE PREPARATION

.1	Thoroughly clean the surface using high-pressure wash with a minimum 34.5 MPa or 24.1 MPa with sand brought into the nozzle.

Specifier Notes:  The pressure gauge must show 34.5 MPa. Note: The original pumps may have been outputting this pressure, but after some wear, the pressure could be considerably lower. When using 34.5 MPa water, the nozzle providing rotating water stream must be used and placed not more than 30 cm from the surface. The surface porosity after cleaning must be clearly visible.  When in doubt, perform a bond test to assure proper surface preparation is being done, or if any additional cleaning or abrasive cleaning is required. If concrete surface is very hard due to a high compressive strength or due to using Zemdrain, (by Dupont) as part of concrete forming, contact Gemite Products Inc. for advice.

.2	Ensure all soft concrete surfaces and any bond-inhibiting materials, such as release agents, are removed.

.3	Wash the surface thoroughly with water prior to the application of the cementitious coating.

.4	Allow all surface water to dry off to achieve a saturated surface dry (SSD) condition.

.5	To ensure proper surface preparation, a bond test should be performed in accordance with manufacturer’s instructions.

.6	Surface Repair

.1	Use thin patching mortar to patch "honeycombing" and air pockets.

.2	Use polymer-modified structural repair mortar for patching in excess of 6 mm.

.3	Uneven concrete, due to concrete form misplacement, must be chipped away and 	surface patched smooth.

.4	Build corner coves 50 mm x 50 mm minimum, using an overhead or vertical 	structural repair mortar.

.7	 Thin Set Concrete Restoration Mortar

Specifier Notes:  Clean the surface of GEM-PLAST TC (finishing plaster) with pressure water in the same manner as cleaning of the concrete surface. Note: Pressure washing the GEM-PLAST TC surface the next day, while the material has not developed a full strength, makes the surface preparation of GEM-PLAST TC for application of CEM-KOTE FLEX ST easier.

.1	Hand application

.1	Apply thjn set mortar using a trowel, in a manner similar to stucco application; 				a “scratch” coat and the second (third) coat, and finish using a float, to obtain 				an “open structure” surface.

.2	Spray Application

.1	Apply first a thin “scratch” coat and brush the surface to obtain continuity.

.2	Apply the second (third) coat – “wet to green condition.”

.3	Compact the material using a trowel to eliminate entrapped air and finish with 				float to obtain “open structure” surface.

Specifier Notes:  If GEM-PLAST TC layer must be left overnight prior to application of consecutive coat, leave the surface “rough” and pressure wash with a minimum 24 MPa water.

.3	Air dry cure GEM-PLAST TC for a minimum three days prior to application of flexible 			cementitious coating.

.8	Treatment of Existing Cracks and All Non-Structural Joints

Specifier Notes:  In some underground projects, the concrete wall/slab might be completely saturated with water. The water-leaking cracks indicate this situation. Alternatively, the general information about the structure also indicates the possibility of “water head” behind wall or below the slab. In such situation, use a strip of REINFORCING FABRIC HD, instead of REINFORCING FABRIC NW, to treat the cracks to allow better drying/curing of CEM-KOTE FLEX ST over the crack. The active water-leaking crack must be sealed using either “cut and fill method” with hydraulic water plugs or by urethane injection. The crack must be free of water leaks for at least three days to allow the CEM-KOTE FLEX ST to cure/dry over the cracks and become watertight.

.1	Identify all the existing cracks and joints and apply a thin layer of the flexible cementitious coating approximately 115 mm wide and 0.5 mm (19 mils) thick by trowel or brush.

.2	Embed the non-woven reinforcing fabric over the entire area of this coating and work 	in using trowel.

.3	Ensure this coating application totally covers the reinforcing fabric.

.4	Let dry sufficiently and apply an additional coat of this flexible cementitious coating 	to build up to a total thickness of 1 mm (38 mils) over the entire area.

.9	Treatment of Inside Corners

.1	Install a 50 mm x 50 mm cove over the inside corners using polymer-modified structural repair mortar.

.2	Apply a thin layer of flexible cementitious coating approximately 254 mm wide 	and 0.8 mm (31 mils) thick by trowel or brush.

.3	Embed the woven reinforcing fabric over the entire area of this coating and work in 	using trowel.

.4	Ensure this coating application totally covers the reinforcing fabric.

.5	Apply an additional coat of this flexible cementitious coating to build up a total 	thickness of 1.6 mm (63 mils) over the entire area.

.10	Treatment of Protruding Elements

.1	Apply two coats of flexible cementitious coating at a thickness of 1.6 mm (63 mils) to 	both the concrete surface and protruding element.

.2	Form a 50 mm x 50 mm minimum cove using polymer-modified structural 	repair mortar in the corner.

.3	Allow the polymer-modified structural repair mortar to cure.

### Specifier Notes: In case the concrete structure is less than six weeks old after casting concrete and the drying shrinkage cracking had not yet occurred, REINFORCING FABRIC HD should be used throughout, since it is unknown where the cracks will be formed. The REINFORCING FABRIC HD fabric is there to allow the maximum crack spanning during the formation of cracks after installation of the membrane. When applying REINFORCING FABRIC HD over the entire surface, use the same procedure as described in 3.2.9. Overlap the fabric by a minimum of 2.54 cm. Avoid “sharp” corners. Apply MEADOW-CRETE OV into the corner to form a “cove” (gradual transfer from one side to the other side of the corner).

Specifier Notes: In existing facilities, REINFORCING FABRIC HD is used only over the existing (non-structural, typically drying shrinkage) cracks, cold (construction) joints. Use a strip of REINFORCING FABRIC HD over any coved corners. The expansion joints must be respected.

Specifier Notes:  When using CEM-KOTE FLEX ST in ozone treatment tanks of potable water facilities, REINFORCING FABRIC HD is used on the entire surface and the minimum thickness of CEM-KOTE FLEX ST system must be 2 mm (79 mils).

3.3		MIXING

### .1	Mix the content of the bag, component A, with the liquid component B.

### .2	Use a heavy-duty drill (400 - 600 RPM) with a helix screw or paddle mixer to achieve thorough mixing.

### .3	Pour approximately 80% of the liquid component B into the mixing container (mixer) and gradually add the dry component A into the liquid and mix until a smooth and lump-free mix is obtained.

### .4	Add the remaining liquid as required for a given application consistency.

### .5	At high ambient temperatures, and depending on application, one to two cups (300-400 mL) of water can be added if required.

3.4		APPLICATION

### .1	Application

### .1	Brush or spray apply the first coat of cementitious coating to a thickness of 0.8 mm.

### .2	If spraying, brush the first coat to eliminate any pinholes.

### .3	Apply the second coat after approximately 15 - 30 minutes at the same thickness as 	the first coat (0.8 mm), giving a finish thickness of 1.6 mm.

### .4	Brush the second coat to eliminate pinholes.

### .5	Protect against surface water evaporation.

### Specifier Notes:  If the first coat is left to dry overnight or longer, use 24 MPa to clean the surface before application of an additional coat.

### .2	 Finishing

### .1	To obtain a smooth surface, if required, finish the surface using a steel trowel.

### .3	Curing

### .1	Air-dry cure flexible cementitious coating for 72 hours at 20o C and 70 – 80% 				RH prior to filling with water.

### .2	Allow for longer curing/drying time will be required with cooler temperatures and a 			higher relative humidity.

### Specifier Notes:  Use electrical (NOT propane) heaters or hot air generators to avoid carbonation and carbonation cracking.

### 3.5		SITE CLEANUP

### .1	Remove all excess and waste materials from the jobsite in accordance with contract provisions.

### .2	Ensure all surrounding areas where the material has been applied and is free of debris.

END OF SECTION